# PART 1 - GENERAL

1.1	RELATED DOCUMENTS:

A. 	This specification has been developed to insure the quality of design expected by the Pinellas County School District. Material manufacturers not listed should submit literature, physical samples and installation list of proposed product for review by the P.C.S.B. representative.

B. 	Drawings and general provisions of Contract, including Division 01 General Requirements apply to this Specification.

1.2. 	SCOPE:  Sanding and refinishing of existing Gymnasium, Basketball/Volleyball courts.

1.3 	QUALITY ASSURANCE:

A. 	Material supplier shall be a firm established in the industry.

B. 	Flooring contractor shall be a company with a minimum of three (3) years continuous experience in the athletic flooring field. A list of at least three completed projects of similar magnitude and complexity where this work has been performed shall be submitted all with submittals/proposals. For each completed project owner references including contact information of a person with direct knowledge of the work shall be included.

Manufacturers wishing to gain prior approval shall request, in writing, the owner’s qualification criteria.

1.4  	SUBMITTALS:

A. 	Submit three copies of manufacturer’s product data.

B. 	Samples:  Upon request of Pinellas County Schools, physical samples may be required for review.

C. 	Maintenance Literature: Three copies of MFMA Care and Maintenance of wood floors.

D. 	Certification:  Manufacturer shall provide certification that all materials meet grade, quality and treatment if applicable.

1.5  	DELIVERY, STORAGE AND HANDLING:

Materials shall not be delivered to the jobsite until all masonry, painting, plastering, tile work, work is complete. Where other trades are involved, all overhead mechanical work, lighting, backstops, and scoreboards shall be installed. Room temperature shall be 55-80 degrees and a consistent relative humidity maintained.

1.6 	JOB CONDITIONS/SEQUENCE:

A. 	Do not commence work until requirements listed in the previous paragraph are obtained.

B. 	Permanent heat, light, and ventilation shall be operating and maintained during and following installation.

C. 	After floors are finished, area is to be locked by School representative to allow time for curing of the finish.  Owner shall protect finished floor until inspection and acceptance.

PART 2 - PRODUCTS

2.1 	MANUFACTURERS:  The following manufacturers' products have been used to establish minimum standards for materials, workmanship and function:

Buckeye Reflections:

2.2 	Equal products from other manufacturers may be used in the work provided such products have been approved, by the Architect of record, not less than ten (10) days prior to scheduled bid opening.

2.3 	Materials:

## A. 	GYM SEALER:	Buckeye Coliseum 100 Oil-Modified Urethanes

B. 	GYM FINISH:	Buckeye Arena 300 Water-Based Urethanes

1) 	Physical Characteristics:

2) 	Gloss Level:	 (60°) 90+

3) 	Solids:	 30 + 1%

4) 	Density:	8.5 lbs/gallon

5) 	VOC:	Does not exceed 450 grams per liter (3.8 pounds per gallon)

C. 	GAME LINE PAINT:  B COURTLINES Game line Paint is Acceptable Manufacturer’s standard colors.

1) 	Benjamin Moore Impervo Alkyd High Gloss Enamel. Or Impervex Latex Hi-Gloss

2) 	Sherwin Williams Industrial & Marine Enamel. Or Industrial & Marine Coatings DTM Acrylic/

3) 	Porter Glyptex Urethane Enamel

PART 3 - EXECUTION

3.1  	FLOOR INSPECTION:

A. 	Inspect existing subfloor floor for proper dryness and tolerance and report any discrepancies to the owner’s representative in writing. It is the intent of the owner to make necessary repairs where deficient materials are discovered. Any floor repair will be approved by the owner’s representative prior to performance of the work. Additional cost associated with this floor repair shall be addressed with the flooring contractor via a Change Order using “unit cost” provided on the original bid form proposal.

B. 	All floor repairs must be performed and complete prior to the refinishing of the maple flooring.

3.2 	REFINISHING - Make sure floor is free of moisture.

A. 	Sweep floors clean.

B. 	Remove all tape and gum with a putty knife or scraper

C. 	Sand with heavy, power driven type sander.  Use dust accumulator on machine.

D. 	Sand with No. 40 or 36 grit sandpaper if boards are uneven heights. First pass shall be on a diagonal angle to the direction of the floor.

E. 	Make sure floor is sanded smooth and level before sanding with medium grit (50 or 60 grit) sandpaper. This cut and all subsequent cuts shall be sanded in the direction of the grain of the floor.

F. 	Sand edges with No. 60 or 80 grit spinner paper.

G.	Sand entire floor with No. 80 or 100 grit sandpaper.

H. 	Disk sand entire floor with No. 100 disk paper.

I. 	Scrape and hand-sand corners and other areas not reached by machine.

J. 	Clean floor to remove all dust and debris prior to sealing wood. Floor shall be smooth and free of shiners.

3.3 	FINISHING:

A. 	Tape off and protect all Volleyball Sleeve covers

B. 	Apply two coats of Coliseum 100 gym sealer.

C. 	Game lines, logos, and lettering shall be placed on floor after screening of seal coats.

D. 	Comply with all local sports jurisdictions when applying lines.

E. 	Color shall be selected by the owner’s representative from standard colors. See Floor plan for special game lines and graphics to be applied to the floor.

F. 	Game lines shall off gas for 36 to 48 hours before screening and finish coats

G.  Apply First Coat of Arena 300 Floor Finish with a light weight T-bar applicator going with the grain. Do Not Puddle Finish

H. 	Apply Second Coat of Floor Finish (Arena 300) with lightweight T-bar applicator going with the grain. Do Not Puddle finish.

I. 	Let Floor dry approximately 2 hours to tack free. Then allow at least 4 hours but not more than 16 hours after tack free before recoating

J. 	Apply Third & Final Coat of Floor Finish (Arena 300).

K. 	Close doors and windows, turn off vent fans and Air Conditioning to avoid excess and direct air while coating.

3.4 	PERIMETER MOLDING:

A. 	Install vented rubber base (where missing) at all walls with adhesive.

B. 	Use pre-formed outside corners and neatly miter all inside corners.

3.5 	CLEAN UP:

A.  Remove all sanding dust from job site. (Do not use the School dumpster)

B. 	Clean and dust off Bleachers, wall padding, doors and base trim before finish coats are applied.

C. 	Check the operation of all bleachers, clean and dust off debris from wheels.

D. 	Clean and check the operation of all volleyball sleeve covers and any low voltage floor mounted boxes.

3.6 	STAGE FLOORS

A. 	After sanding apply two (2) coats of Sealer.

B. 	For High School Working Stage floors apply two (2) of finish with a Matting agent.

3.7 	DANCE FLOORS

For Dance floors application of Matting agent is optional with approval of the PCSB Project Manager.

END OF SECTION